October 21, 2010

# REVISION OF SECTIONS 612, 614, 630, and 713

RETROREFLECTIVE SIGN SHEETING

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions regarding its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies that use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on all projects.

October 21, 2010

REVISION OF SECTIONS 612, 614, 630, and 713

## RETROREFLECTIVE SIGN SHEETING

Sections 612, 614, 630, and 713 of the Standard Specifications are hereby revised for this project as follows:

In subsection 612.02 (a) 2.C., first paragraph, delete the last sentence and replace with the following:

Reflective material shall be Type IV reflective sheeting meeting the requirements of subsection 713.10.

In subsection 614.07, first paragraph, delete the second sentence and replace with the following:

Retroreflective sheeting shall be type IV and shall conform to subsection 713.04.

In subsection 630.06, first paragraph, delete the fifth sentence and replace with the following:

Reflective sheeting on new devices shall be Type IV. Existing devices manufactured with Type III sheeting may be used on projects advertised prior to January 1, 2014.  Devices used on projects advertised on or after January 1, 2014 shall be manufactured with Type IV sheeting.

In subsection 713.06, third paragraph, delete the second sentence and replace with the following:

The background retroreflective sheeting shall be Type IV.