Sample Project Special Provision: 703mf

(Pilot Spec to be used as directed by the Region Materials Engineer)

Page 1 of 1

11-30-06

REVISON OF SECTION 703

MINERAL FILLER

Section 703 of the Standard Specifications is hereby revised for this project as follows:

Subsection 703.06 shall include the following:

If mineral filler other than limestone dust is used in Stone Matrix Asphalt (SMA) it shall consist of mineral matter that meets the requirements of Table 703-7 and the following:

Alternate mineral filler shall consist of finely divided mineral matter such as rock dust, slag dust, fly ash, loess, or other suitable mineral matter. Calcium Oxide content of any mineral filler shall not exceed 22 percent.

Production will be suspended if alternate mineral filler test results fail to meet requirements. The Contractor shall submit plans to correct the mineral filler operation to the Engineer for approval prior to commencing paving.

Alternate mineral filler test data shall be provided at SMA mix design submittal and as required during production.

Table 703-7

Required Testing for Alternate SMA Mineral Fillers

| Type of Test | Testing Frequency | Specification Limit | Remarks |
| --- | --- | --- | --- |
| Plasticity Index AASHTO T90 | One per 10,000 tons of SMA placed♦ | 4% Maximum | ▲ |
| Hydrometer Analysis AASHTO T88 | One at Mix Design submittal | Report |  |
| Gradation AASHTO T37 | One per 10,000 tons of SMA placed♦ |  | ▲ |
| Calcium Oxide Content ASTM C25 | One at Mix Design submittal | 22% Maximum |  |
| Modified Rigden Voids – NAPA Publication IS-101 | One per 10,000 tons of SMA placed♦ | Shall not exceed 50 | ▲ |
| ♦ The minimum frequency shall be twice per project ▲ Sampling of alternate mineral fillers shall be at the point of introduction to the SMA and a split sample shall be submitted to the Engineer |

| Alternate SMA Mineral Gradation Criteria (AASHTO M17/ASTM D 242-95) |
| --- |
| Sieve | Percent Passing |
| 600 (#30) | 100 |
| 300 (#50) | 95 - 100 |
| 75 (#200) | 70 - 100 |