# Sample Project Special Provision 208dfb

10-25-07

REVISION OF SECTION 208

Dewatering Filter Bags

Section 208 of the Standard Special Provisions is hereby revised for this project as follows:

Subsection 208.01 shall include the following:

This work consists of furnishing, placing, securing, maintaining, and replacing filter bags for dewatering as required.

Subsection 208.02 shall include the following:

- Dewatering Filter Bags. Filter bags shall be made of UV resistant, non woven geotextile sewn into a large, completely enclosed bag. Filter bag shall be sized to accommodate the dewatering operation rate of discharge. Each filter bag shall have the following properties:

| Tensile Strength | 200 to 260 lbs. | ASTM D 4632 |
| --- | --- | --- |
| Puncture Strength | 120-160 lbs. | ASTM D 4833 |
| Mullen Burst | 360-550 psi | ASTM D 3786 |
| AOS | 100 sieve | ASTM D 4571 |
| Water Flow Rate | 85-110 gpm/ft2 | ASTM D 4491 |
| UV Resistance | 70%@ 500 hrs | ASTM D 4355 |

Subsection 208.05 shall include the following:

- Dewatering Filter Bags. Dewatering filter bags shall be placed on a level, stable surface, consisting of pavement, grass or aggregate. Dewatering filter bags shall not be placed within a wetland or in open water. Discharge water shall not cause erosion. Discharge water shall be free of sediment or other pollutants.

Dewatering filter bags shall be maintained or replaced when full to capacity.

The pump discharge hose shall be installed into the dewatering filter bag spout and secured with a strap. One discharge hose shall be installed per bag. Filter bags shall be capable of collecting and filtering sediment from pumped water.

Subsection 208.08 shall include the following:

Dewatering Filter Bags will not be measured and paid for separately, but shall be included in the work.