# October 25, 2007

REVISION OF SECTION 703

AGGREGATE FOR BASES

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on all projects having Aggregate Base Course (Class 3).

October 25, 2007

REVISION SECTION 703

AGGREGATE FOR BASES

Section 703 of the Standard Specifications is hereby revised for this project as follows:

In subsection 703.03, delete Table 703-3 and replace with the following:

Table 703-3

CLASSIFICATION FOR AGGREGATE BASE COURSE

| Sieve Size | Mass Percent Passing Square Mesh Sieves |
| --- | --- |
|  | LL not greater than 35 | LL not greater than 30 |
|  | Class 1 | Class 2 | Class 3 | Class 4 | Class 5 | Class 6 | Class 7 |
| 150mm (6”) 100mm (4”) 75mm (3”) 60mm (2 1/2”) 50mm (2”) 37.5mm (2”) 25mm (1”) 19mm (3/4”) 4.75mm (#4) 2.36mm (#8) 75mm (#200) | 100 95-100 30-65 3-15 | 100 95-100 3-15 | 100 20 max | 100 90-100 50-90 30-50 3-12 | 100 95-100 30-70 3-15 | 100 30-65 25-55 3-12 | 100 20-85 5-15 |
| NOTE: Class 3 material shall consist of bank or pit run material. |