# MEMORANDUM

# DEPARTMENT OF TRANSPORTATION

Project Development Branch

# 4201 East Arkansas Avenue

Denver, Colorado 80222

(303)757-9040

FAX (303)757-9868

# DATE:	October 25, 2007

# TO:	All Holders of Standard Special Provisions

# FROM:	Larry Brinck, Standards and Specifications Engineer

# SUBJECT:	Revision of Section 712, Hydrated Lime

# As of this date, our unit is issuing a new standard special provision, Revision of Section 712, Hydrated Lime. This standard special is 1 page long, and is dated October 25, 2007.  It is to be used on projects having Hot Mix Asphalt (HMA) or Stone Matrix Asphalt (SMA).  While the use of this standard special provision is required on projects advertised on or after November 22, 2005, you are free to use it on projects advertised before this date.

# This new standard special provision modifies CDOT’s current specification for hydrated lime used in HMA or SMA from ASTM C 207 Type N to AASHTO M 303 Type I, since it was determined that there was no significant difference in moisture susceptibility between 80 percent fines passing the #200 sieve, and CDOT’s standard method of 90 percent passing #200 sieve.

# Those of you who keep books of standard special provisions should add this new standard special provision to your file. For your convenience, a new Index of Standard Special Provisions dated October 25, 2007 is attached.

# mrs/dvdw

# Attachments

# Distribution: Per distribution list