# November 3, 2008

REVISION OF SECTION 105

CONFORMITY TO THE CONTRACT OF HOT MIX ASPHALT

## NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions regarding its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies that use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects if the project has more than 5000 Tons of Hot Mix Asphalt (HMA) and the project is NOT a voids acceptance project.

November 3, 2008

REVISION OF SECTION 105

CONFORMITY TO THE CONTRACT OF HOT MIX ASPHALT

Section 105 of the Standard Specifications is hereby revised for this project as follows:

Subsection 105.05 (f) shall include the following:

If removal and replacement is required because the joint density PF for a process is below 0.75, the Contractor shall remove and replace the full lane width adjacent to and including at least 6 inches beyond the visible joint line for the entire length of joint representing the process.  If the lane removed is adjacent to another joint, that joint shall also be removed to a point 6 inches beyond the visible joint line.  When a single joint density core is more than 2V outside the tolerance limits, the removal and replacement limits shall be identified by coring the failing joint at 25 foot intervals until two successive cores are found to be 1V or less below the minimum tolerance limit. If removal and replacement is required, the Contractor shall submit documentation identifying the process to be used to correct the area in question in writing. The process will be approved by the Engineer before commencing the corrective work.