## April 30, 2009

REVISION OF SECTION 307

# LIME TREATED SUBGRADE

#### NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions regarding its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies that use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects having Item 307, Lime Treated Subgrade.

April 30, 2009

REVISION OF SECTION 307

LIME TREATED SUBGRADE

Section 307 of the Standard Specifications is hereby revised for this project as follows:

Delete Table 307-1 and replace with the following:

TABLE 307-1

# SCHEDULE FOR MINIMUM SAMPLING AND TESTING

| Element and Procedure | Process Control | Acceptance | Remarks |
| --- | --- | --- | --- |
| pH ASTM C 977 (App) (Design) ASTM G 51 (Field) | 1/5,000 sq. yds. or fraction thereof | 1/10,000 sq. yds. or fraction thereof | pH will be determined after % lime has been established based on unconfined compressive strength |
| Atterburg Limits AASHTO T 89, T 90 | 1/5,000 sq. yds. or fraction thereof | 1/10,000 sq. yds. or fraction thereof | Reduce by ½ original PI |
| Swell Potential ASTM D 4546 | 1/5,000 sq. yds. or fraction thereof | 1/10,000 sq. yds. or fraction thereof | ½% or less with 200 psf surcharge pressure Modified as per local practices |
| Unconfined Compressive Strength ASTM D 5102 (Procedure B) | 1/5,000 sq. yds. or fraction thereof 1/soil type | 1/10,000 sq. yds. or fraction thereof 1/soil type. | Determined by design plan criteria Do not immerse in water after moist-cure period. The tests shall be conducted on samples cured in a moist environment for 5 days @ 100 F |
| Thickness Acceptance ASTM C 174 | A lot is defined as 1 core per 1,500 sq. yds. or fraction thereof | 1/3,000 sq. yds. or fraction thereof | When measurement is <0.5”, 2 additional cores shall be taken in that lot and the average of 3 cores will determine the thickness of that lot |
| Gradation AASHTO T11 and T27 | 1/5,000 sq. yds. or fraction thereof | 1/10,000 sq. yds. or fraction thereof | 1” – 100% passing #4 – 60% passing Dry sieving after final mixing |
| Determining Percent Relative Compaction Soil-Aggregate by Nuclear Method CP 80 | 1/5,000 sq. yds. or fraction thereof | 1/10,000 sq. yds. or fraction thereof | Minimum 95% of maximum dry density as per AASHTO T 99. Moisture content of mixture at the start of compaction shall be at 2 ± 1% above optimum moisture content |
| Moisture Density Curve AASHTO T 99 | 1/soil type | 1/soil type |  |
| Sulfate CP-L 2103 | 1/soil type | 1/soil type | Water soluble sulfate content in soil shall be less than 0.2% by dry soil weight. |