NOTICE

This is a project special provision that revises or modifies CDOT’s *Standard Specifications for Road and Bridge Construction*. It has gone through a formal review and approval process and has been issued by CDOT’s Construction Engineering Services Branch with formal instructions for its use on CDOT construction projects. It is to be used as written without change. Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit. The instructions for use on CDOT construction projects appear below.

Other agencies which use the *Standard Specifications for Road and Bridge Construction* to administer construction projects may use this special provision as appropriate and at their own risk.

**Instructions for use on CDOT construction projects:**

Use this standard special provision on all projects with structural concrete.

Revise Section 601 of the Standard Specifications for this project as follows:

Revise Subsection 601.05, second paragraph as follows:

(11) For air entrained concrete, report the SAM number according to AASHTO TP118 Characterization of the Air-Void System of Freshly Mixed Concrete by the Sequential Pressure Method (Super Air Meter). The SAM meter readings for each step shall be included. Perform a SAM leak test prior to the SAM testing. Results of the leak test shall be included in the SAM data.