**NOTICE**

This Standard Special Provision (SSP) revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction. These are the official instructions for its use on CDOT construction projects, and the Construction Engineering Services Branch has reviewed, approved, and issued it. Use as written without change. Do not use modified versions of this SSP on CDOT construction projects. Do not use this special provision on CDOT projects in a manner other than specified in the instructions without approval by CDOT’s Standards and Specifications Unit. The instructions for use appear below.

Other agencies using the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision appropriately and at their own risk.

**Instructions for use on CDOT construction projects:**

Use this standard special provision on all projects.

**Revise Section 627 of the Standard Specifications as follows:**

**Revise Table 627-1 of the Standard Specifications as follows:**

**Table 627-1**

**MINIMUM AND MAXIMUM RANGES OF PAINT AND STRIPES**

| **Description** | **Units** | **Pavement Marking Paint Low Temp** | **Pavement Marking Paint High Build** | **Pavement Marking Paint High Build****(Temporary)** |
| --- | --- | --- | --- | --- |
| Alignment | Lateral Deviation | 2.0 inch per 200 feet Max | 2.0 inch per 200 feet Max | 2.0 inch per 200 feet Max |
| Coverage Rate | Sq Ft per Gallon | 89-93 | 67-70 | 100-105 |
| Thickness | Mil | 17-18 | 23-24 | 15-16 |
| Width | Inches | Per Plans ± 0.25 | Per Plans ± 0.25 | Per Plans ± 0.25 |
| Dry Time | Minutes | 5-10 | 7-12 | 5-10 |
| Beads | Application Rate, lbs./gal | 7-8 | 9-10 | 7-8 |

(6) High Build (Temporary) shall only be used for temporary pavement marking applications.

**Add to subsection 627.13 of the Standard Specifications as follows:**

**627.13** The accepted quantities will be paid for at the contract price per unit of measurement for each of the pay items listed below that appear in the bid schedule.

Payment will be made under:

**Pay Item** **Pay Unit**

Pavement Marking Paint (High Build) (Temporary) Gallon